MATERIAL	TEST	REPORT

.	,

ISO	9001:2008 Certified	I

SOLD TO:	'

rSHIP TO:	'

| Heat Number | Product Description | Certificate No | Certificate Date" |
| --- | --- | --- | --- |
| 1420763X | ROD CMI-C IRON ROD CD 1-3/4" DIA X 1 foot |  |  |

| Sales Order | Salesperson | Customer PO | Contact | Country Of Origin | \ |
| --- | --- | --- | --- | --- | --- |
|  | ELIZABETH BOZZUTO |  |  |  | J |

Chemical Analysis (Weight %)

| C | Mn | Si | P | S | Cr | Ni | V | Ti | A1 |  | Fe |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| .0100 | .1600 | .0040 | .0030 | .0060 | .0100 | .0200 |  |  | .0060 |  | Balance |

Mechanical Properties

| Yield Strength | Tensile Strength | % EL | % RA | Hardness | Grain Size^ |
| --- | --- | --- | --- | --- | --- |
| 44,256 PSI (305.13 MPA) | 53,188 PSI (366.72 MPA) | 29% |  | RB 85.0 |  |

Other Tests / Remarks

ASTM A848-ALLOY 1

We Certify that this material is DFARS 252.225-7014 and RoHS 2 Directive 2011/65/UE Compliant. This material is Mercury Free.

Quality Control Manager:    J. Bozzuto    Date:	12/13/16