MATERIAL	TEST	 REPORT

ISO9001:2008 Certified	1001435

| r SOLD TO: |  |
| --- | --- |

| SHIP TO: |  |
| --- | --- |

| Heat Number | Product Description | Certificate No | Certificate Date ' |
| --- | --- | --- | --- |
| 1584563 | ROD CMI-C IRON ROD CD 1/2" DIA X 1' |  | .J |

| Sales Order | Salesperson | Customer PO | Contact | Country Of Origin " |
| --- | --- | --- | --- | --- |
|  | ELIZABETH BOZZUTO |  |  |  |

Chemical Analysis (Weight %)

| C | Mn | Si | P | S | Cr | Ni | V | Ti | A1 |  | \ Fe |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| .0100 | .1700 | .0220 | .0060 | .0070 |  |  |  |  | .0020 |  | Balance |

Mechanical Properties

| r Yield Strength | Tensile Strength | % EL | % RA | Hardness | Grain Size" |
| --- | --- | --- | --- | --- | --- |
| 52,648 PSI (362.99 MPA) V _ | 53,373 PSI (367.99 MPA) | 21% |  | RB 85.0 |  |

Other Tests / Remarks

ASTM A848-ALLOY 1

We Certify that this material is DFARS 252.225-7014 and RoHS 2 Directive 201 1/65/UE Compliant. This material is Mercury Free.

Quality Control Manager:  J. Bozzuto	     Date: 12/13/16